σij2=δB2∙corrij+δbroad∙rij2+δg∙rij2

where

δB2=B4π2

is the atomic mean square displacement, with B=BISO, but it is also possible to use Bij;

corrij=1-λij,k for k<Nk1-δ1rij,k-δ2rij.k2 for k≥Nk

with Nk as the coordination shell number;

δg=δg, constant for a Gaussian microstrainρ∙b24 π2Γhkl∙f*rijRe for a microstrain caused by dislocations

with

- b = √3/2·a (Burgers vector modulus of bcc Fe, a is the unit cell parameter)
- Γhkl is the average contrast factor:
  Γhkl=fE∙CEdge+1-fE∙CScrew 
with fE as the fraction of edge dislocation and CEdge and CScrew the average contrast factors for edge and screw dislocations, respectively. The average contrast factor for cubic systems is

Cx=A+B∙H

with x=Edge, Screw, A and B are constants depending on elastic tensor and dislocation slip system, whereas

H=h2∙k2+k2∙l2+l2∙h2h2+k2+l22   
- f* is the Wilkens function:
  - for rij/Re ≤ 1: f* = -ln(x) + 7/4 - ln(2) + x²/6 - 32x³/(225π)
  - for rij/Re > 1: f* = 512/(90πx) - (11/24 + 0.25ln(2x))/x²